Driveseal

DESCRIPTION

Driveseal is a single pack, solvent-borne, clear Acrylic resin based curing compound, surface sealer and dust proofer for concrete and block paving. When applied to freshly placed concrete,  Driveseal functions as a curing membrane, reducing any tendency towards drying shrinkage cracks. At the same time the surface becomes sealed against the ingress of oils and many aqueous chemicals, and a harder wearing floor is produced. When applied to old/aged concrete floors,  Driveseal penetrates into the pore structure thereby sealing and dust proofing the surface.

USES

As a curing/sealing treatment to new concrete.

As a sealing/dust proofing treatment to old concrete and blocks to provide a sealed and dust-proof surface with resistance to the ingress of oil, petrol and chemical spillages.

ADVANTAGES

Easily applied by brush, roller or spray

Good chemical and abrasion resistance

Seals and dust proofs the surface

Provides easily cleanable floor surface

Internal and external use

Resistant to ultra violet radiation

Single pack – ready to use

PROPERTIES

Appearance:   Pale straw coloured liquid with characteristic odour

S.G.:  0.910g/cm³

Drying time @ 20°c:

Tack free 2-4 hours

Hard dry 16-24 hours

Flash point:  40°c

Chemical resistance:  Resistant to spillages of dilute mineral acids, caustic alkali solutions, vegetable oils, de-icing salts, etc.

Procedure

Surface Preparation

Old concrete and block paving  shall be sound and free from oil, grease, laitance and other contaminants.  Previously applied paint or curing membrane must be removed.  Wash the floor with a detergent solution followed by a clean water wash, and then allow to dry prior to sealer application.

New concrete.  Driveseal may be applied 15 minutes after the final power float or brush finish.

APPLICATION

Old concrete.  Apply a coat of  Driveseal by brush, roller, squeegee or spray at a nominal rate of 8-9m²/litre.  Avoid the formation of puddles of excess material.  After a minimum period of 16 hours a second coat shall be applied at a rate of 11-12m²/litre

NOTE:  On very porous substrates a third coat may be necessary

New concrete.  Apply  Driveseal by spray at a nominal rate of 5m²/litre.  Ensure that the material is applied evenly and avoid the formation of puddles of excess material on the surface.  In hot and/or windy conditions, a second coat of  Driveseal should be applied the following day at a nominal rate of 8-10m²/litre

Block Paving.  Ensure enough material is applied to fully seal the surface.  Coverage is dependent on the porosity of the block.

EQUIPTMENT CLEANING

Clean equipment with  Toolclean  prior to curing of the coating.

CURING

Driveseal wil be tack free in 2-4 hours and hard dry after 16-24 hours in conditions of good ventilation.

COVERAGE

Coverage is very much dependent on the porosity of the substrate.

New concrete. Typical application rate is 5m²/l (one coat): a second coat is recommended under fast drying ambient conditions.

Old concrete.  For smooth, power floated concrete, the typical application rate is: 8-9m²/l (1st coat) 11-12m²/l (2nd coat) i.e. overall rate = 4.6-5.1m²/l(two coats)

Block Paving.  Dependent on the type of block, typically 2-4m²/ltr

If a slip resistant finish is required, incorporate Resbuild Texturing Additive and apply only 1 coat of Resbuild Driveseal at a rate of 5m²/litre.  Textured and tamped finishes reduce the coverage rate achieved.

NB.  It is strongly recommended that a small test application be carried out to determine the precise coverage rate for each specific job, prior to any large scale application being started.

STORAGE AND SHELF LIFE

Store in dry conditions, out of direct sunlight, at temperatures between 10°C and 25°C.

Resbuild Driveseal has a minimum shelf life of 12 months when stored in original, unopened containers in accordance with manufacturer’s instructions.

PACKAGING

Driveseal is supplied in 25L packs.

LIMITATIONS

Apply only in well ventilated areas.

Do not apply externally if rain is likely during application or within 6 hours thereafter.

HEALTH AND SAFETY (see separate health and safety data sheet)

Driveseal is a flammable material (flash point = 40°c)

Avoid contact of the material with skin and eyes.

Provide good ventilation during application and wear suitable organic vapour respirators.

Please refer to Material Safety Data Sheet for additional information

Driveseal shall be applied strictly in accordance with the manufacturer’s instructions

For specific advice regarding any aspect of this product, please consult our Technical Department.

WARRANTY DISCLAIMER

The technical data herein has been compiled for your help and guidance and is based upon our experience. As we have no control over the use to which our information is put, no warranty, expressed or implied is intended or given and we cannot be held responsible for coverage, performance or any damages incurred.

Kestral Construction Products Limited – St. Helens, WA9 4HY, 01744 830001: DATA S/781998